5-04.3(10)A	General
(March 9, 2016 APWA GSP)

Supplement this section with the following:

Pneumatic tire rollers shall not be used for compaction of PHMA/PWMA.

The Contractor shall develop a roller pattern that will initially consolidate the pavement structure as well as target 15% to 18% final air voids (82% to 85% of maximum theoretical (Rice) density). The Contractor shall monitor compaction during placement of PHMA/PWMA with a pavement density gauge.